## Slide 1: QuantiCorp R&D Plenary

## Slide 2: Identify the problem
Develop a glucose sensor based on a conducting polymer

## Slide 3: Plan
Literature research
Possible solution
Evaluation
  Research into synthetic methods;
  Functionalization of the polymer;
  Synthesis of the polymer;
  Laboratory pilot study;
  Conjugation with a sensing molecule
Final solution

## Slide 4: Solution
Conjugation of glucose oxidase (GOD) with end functionalised polyacetylene

## Slide 5: Laboratory Study ROMP of COT with a TBS-protected cis-2-butene diol
2
5
1
4
Notes: The reaction scheme for ROMP of COT with a CTA is given in Scheme 2 from Scherman et al. (J. Am. Chem. Soc, 2003, 125, 8515):
Scherman, O. A., Rutenberg, I.M., and Grubbs, R.H.Direct Synthesis of Soluble, End-Functionalized Polyenes and Polyacetylene Block Copolymers. J. Am. Chem. Soc, 2003, 125, 8515
The main advantages of the Grubb’s 2nd generation catalyst (1) used here are that it has a high degree of functional group tolerance and it can be used to polymerize COT (2) which has a low ring strain.

## Slide 6: Results of Laboratory Study
Yield
Qualitative analysis
Notes: From Table 1 in Scherman et al. (J. Am. Chem. Soc, 2003, 125, 8515) the yields were:
Best: [COT]/[CTA] = 2; [COT]/catalyst = 500; yield = 83 %
Worst: [COT]/[CTA] = 3; [COT]/catalyst = 1050; yield = 9 %
Results of the qualitative analysis should be similar to e.g. a typical 1H NMR spectrum shown in Figure 2 from the paper by Scherman et al. (J. Am. Chem. Soc., 2003, 125, 8515) NMR spectrum of TBSO functionalized polyacetylene in CD2Cl2 (from Scherman, O. A., Rutenburg, I.A., and Grubbs, R.H., J. Am. Chem. Soc., 2003, 125, 8515).
There are 8 polyene backbone protons (Ha) at δ = 6-7 ppm for every 4 double bonds, or each molecule of COT, incorporated into the polymer chain; and 4 allylic CH2 protons (Hd) around δ = 4.2 ppm regardless of the polymer chain length.
Hence the number of double bonds (b) is given by: b = 2Ha/Hd
and the number of monomers (n) by: 2n = Ha/Hd
Using the spectrum for reaction 4 given in Resource 7.1:
Ha = 20.27 – 24.88
b ~ 10.1 – 12.4
n ~ 2.5 – 3.1
Scherman, O. A., Rutenburg, I.A., and Grubbs, R.H., J. Am. Chem. Soc., 2003, 125, 8515

## Slide 7: Proposed Method 1 Protection of chain transfer agent
protect cis-butene-1,4,-dicarboxylic acid (6) with trimethylsilyl chloride (7)
Notes: In the original reaction scheme cis-butene-1,4,-diol was protected using dimethyl-tert-butylsilyl chloride. However, for subsequent functionalisation with the GOD protein we require either a carboxylic or amine functional group. One solution is to protect cis-butene-1,4,-dicarboxylic acid (6) with trimethylsilyl chloride (7).

## Slide 8: Proposed Method 2 Polymerisation and end-functionalisation

## Slide 9: Proposed Method 3 Deprotection

## Slide 10: Proposed Method 4 Conjugation with GOD

## Slide 11: Evaluation
Benefits
  Selective for glucose
  Requires no special equipment
Risks
  Proposed synthesis has not been tested
  Inactivation of enzyme
  Reduction in polymer conductivity
  Insoluble product