## Slide 1: Nuclear decommissioning: Turning waste into Wealth
The chemistry of cake
Tzany Kokalova
University of Birmingham

## Slide 2: Contents
Yellowcake and its uses.
From uranium ore to yellowcake:
  impurities,
  solvent extraction,
  neutralisation,
  precipitation.
Summary.

## Slide 3: Yellowcake and its uses
Yellowcake refers to a substance produced after purification and concentration of uranium from ore, using acid leaching techniques and consists of ~80% triuranium octoxide (U3O8).
Impure uranium ore consists of UO2, UO3, U3O8 and impurities.
Purification of uranium ore and extraction of U3O8 (yellowcake) comprise the first stage in the cycle that leads to reactor fuel.
Density: 9.6 g/m3 BP: 2878 °C

## Slide 4: Yellowcake extraction 1
Uranium ore crushed & ground
Uranium leached with sulfuric acid
UO2(SO4)3
Solvent extraction: amines in kerosene
(R3NH)4UO2(SO4)3
Ammonium sulfate & vacuum evaporation removes solvents
(NH4)4UO2(SO4)3
Ammonia added  oxidation, precipitation filtration
(NH4)2U2O7
Heating yields concentrated U3O8 (yellowcake)

## Slide 5: Leaching
Uranium ore crushed & ground
Prior to leaching, the crushed ore is heated to ~750 °C to decompose compounds that could effervesce.
Uranium leached with sulfuric acid
Leaching with sulfuric acid (H2SO4):
For the case of (amphoteric oxide) UO3.
UO3(s) + 2H+(aq) → UO22+(aq) + H2O
UO22+(aq) + 3SO42-(aq) → UO2(SO4)34-(aq)
Pitchblende: UO2, UO3 U2O5

## Slide 6: Yellowcake extraction 2
Uranium ore crushed & ground
Uranium leached with sulfuric acid
UO2(SO4)3
Solvent extraction: amines in kerosene
(R3NH)4UO2(SO4)3
Ammonium sulfate & vacuum evaporation removes solvents
(NH4)4UO2(SO4)3
Ammonia added  oxidation, precipitation filtration
(NH4)2U2O7
Heating yields concentrated U3O8 (yellowcake)

## Slide 7: Solvent extraction
Solvent extraction: amines in kerosene
Solvent extraction with tertiary amines in kerosene (note phase change for UO2):
2R3N(org) + H2SO4 → (R3NH+)2SO4
[R = alkyl grouping → CnH2n+1]
2(R3NH+)2SO42-(org) + UO2(SO4)34-(aq) → (R3NH+)4UO2(SO4)34-(org) + 2SO42-(aq)
Loaded solvent is treated to remove impurities.
Impurities (e.g. silica, zirconates) stay in aqueous phase.

## Slide 8: Yellowcake extraction 2
Uranium ore crushed & ground
Uranium leached with sulfuric acid
UO2(SO4)3
Solvent extraction: amines in kerosene
(R3NH)4UO2(SO4)3
Ammonium sulfate & vacuum evaporation removes solvents
(NH4)4UO2(SO4)3
Ammonia added  oxidation, precipitation filtration
(NH4)2U2O7
Heating yields concentrated U3O8 (yellowcake)

## Slide 9: Precipitation & oxidation 1
Ammonium sulfate & vacuum evaporation removes solvents
Addition of ammonium sulfate followed by heating removes solvents:
(R3NH+)4UO2(SO4)34-(org) + 2(NH4)2SO4(aq) →
4R3N(org) + (NH4)4UO2(SO4)3(aq) + 2H2SO4(aq)
Return of acid and amine.

## Slide 10: Precipitation & oxidation 2
Ammonia added  oxidation, precipitation filtration
Precipitation of (NH4)2U2O7 using gaseous ammonia:
6NH3(g) + 2UO2(SO4)34- + 3H2O → (NH4)2U2O7(s) + 2(NH4)2SO4
Return of ammonium sulfate.
Heating yields concentrated U3O8 (yellowcake)
Heating ammonium diuranate precipitate, (NH4)2U2O7, produces U3O8 (yellowcake).

## Slide 11: Yellowcake summary
Additional purification steps before leaching include:
NaCl followed by heating to convert silver to silver chloride.
Addition of NaNO3 to oxidise UO2 to UO3.
Yellowcake is the starting point for UF6 production:
UF6 is used to enrich content of 235U.
UF6 can be converted to UO2 e.g. for AGR/CANDU (reactor fuel).

## Slide 12: Bibliography 1
Sources/further reading
Hurd W. Safford and A. Kuebel, J. Chem. Educ., (1943) 20 (2), p88
Frank Settle, case study: Nuclear Chemistry Uranium .
Production – http://www.chemcases.com
J.M.W. Mackenzie, Henkel Ltd, Uranium Ore Yellow Cake seminar, Melbourne (1997.)

## Slide 13: Bibliography 2
Sources/further reading
World Nuclear Association http://www.world-nuclear.org
Manufacture of Marketable Uranium Compounds – http://www.lookchem.com
Contents page image from the Uranium Information Center

## Slide 14: Copyright information
 Royal Society of Chemistry
Registered charity number 207890
This resource is shared under a Creative Commons Attribution-NonCommercial-NoDerivatives 4.0 International licence
To view a copy of the license, visit https://creativecommons.org