Producing ‘gold’ coins on a microscale

This resource is part of a collection of ideas and activities for chemistry lessons in the festive season. Find more at: rsc.li/3h40uXc.

A student sheet with questions, teacher notes including answers, plus integrated instructions are available at rsc.li/3TZmRLN.

Equipment (per group)

6 V DC source or 9 V battery

2 electrical leads

2 crocodile clips

2 steel paper clips

Petri dish

Measuring cylinder, 10 cm3

Measuring cylinder, 25 cm3

Beaker, 50 cm3

Bunsen burner

Heat proof mat

Tongs

Wash bottle or dropping pipette

Cloth

Copper coin (copper foil can be used if you do not have access to copper coins)

Zinc foil

Sodium hydroxide, 0.4 mol dm-3

Zinc sulfate(VI), 0.1 mol dm-3

- Safety equipment: safety spectacles

Preparation

- Prior to the start of the lesson, clean the copper coins or strips of copper foil. Using plastic forceps, immerse the copper coins or foil in a beaker of warm 0.5 mol dm-3 nitric acid for a few seconds. Rinse the copper coin/strip with water and dry with a cloth.

Equipment set-up

Safety

Read our standard health and safety guidance and carry out a risk assessment before running any live practical.

Refer to SSERC/CLEAPSS Hazcards and recipe sheets.

Hazard classification may vary depending on supplier.

| Chemical supplied for the practical | Preparation |
| --- | --- |
| Nitric(V) acid, 0.5 mol dm-3 HNO3(aq) WARNING Irritant (skin, eyes) May produce toxic fumes | Nitric(V) acid, concentrated HNO3(l) MW = 63.01 g mol-1 DANGER May intensify fire; oxidiser Causes severe skin burns and eye damage Toxic if inhaled Corrosive to the respiratory tract |
| Sodium hydroxide solution, 0.40 mol dm-3 NaOH(aq) WARNING Irritant (skin, eyes) | Sodium hydroxide solid NaOH(s) MW = 40.00 g mol-1 DANGER Causes severe skin burns and eye damage |

| Zinc sulfate(VI), 0.10 mol dm-3 ZnSO4 (aq) WARNING Irritant (eyes) | Zinc sulfate(VI) heptahydrate solid ZnSO4.7H2O (s) MW = 287.54 g mol-1 DANGER Harmful if swallowed Causes serious eye damage Very toxic to aquatic life with long lasting effects |
| --- | --- |
| Sulfuric(VI) acid, 1.0 mol dm-3 H2SO4(aq) WARNING Irritant (skin, eyes) | Sulfuric(VI) acid, concentrated H2SO4 (l) MW = 98.07 g mol-1 DANGER Cause severe skin burns and eye damage |
| Copper coin Cu(s) Currently not classified as hazardous |  |
| Zinc foil Zn(s) Currently not classified as hazardous |  |

Hazards

Wear safety glasses.

Beware of sharp edges when manipulating the zinc foil.

Take care to avoid skin contact with the electrolyte solutions.

Work in a dry area. Make sure that the power supply is switched off when the equipment is put together and that it is switched off again when dismantling.

Hot coins could cause burns. Allow to cool before handling.

Disposal

Dilute the plating solution in a bucket of water and pour down a foul water drain.

Dilute the sulfuric acid solution down to 0.1 mol dm-3 and pour down a foul water drain.

Dilute the nitric acid solution down to 0.1 mol dm-3 and pour down a foul water drain.